## SODA ASH LIGHT

| Sodium carbonate | Na2CO3 | - min 99,5% |
| --- | --- | --- |
| Sodium chloride | NaCl | - max 0,15% |
| Ferric oxide | Fe2O3 | - max 0,0025% |
| Sodium sulphate | Na2SO4 | - max 0,02% |
| Insoluble substances |  | - max 0,02% |
| Loss on ignition |  | - max 0,5% |
| Bulk density |  | - 580-680 kg/m³ |

Sieve analysis:

| > 2.5 mm | - max 1 % |
| --- | --- |
| < 0.4 mm | - min 90 % |

Na2CO3 is  guaranteed by sample roasted

in temperature of 270-300 degrees centigrade.

Information in this publication is believed to be accurate and is given in good faith, but it is for the customer to satisfy itself of the suitability for its own particular purpose.

No representation, warranty or guarantee is made as to its accuracy, reliability or completeness.